# SECTION 0742XX

EXTERIOR RAIN & WIND SCREEN SYSTEMS

# Part 1 	GENERAL

- SCOPE OF WORK

  - Sections Include:

    - Exterior Glass Panels.

    - Aluminum Fittings.

    - Glazing Accessories.

- REFERENCES

Comply with applicable provisions of the following Rain Screen test criteria for design, materials, and installation of component parts:

AAMA 509-09, ASTM E 330-02, ASTM E 283-04, ASTM E 331, ASTM E 331-00, AAMA 501.1-05, DIN 18516 Part 4. Visual characteristics for all fasteners and glass in accordance with glass manufacturer’s product definition.

  - DEFINITIONS

The system provides horizontal or vertical and horizontal overlap glazing panels for a back ventilated system without glass cut-outs or holes.  The system prevents or helps minimize the horizontally driven rain from accessing the building envelope. Overlap fastening system, Bendheim Wall Systems Rainscreen with LängleGlas fastening fittings or equal, with structural engineering calculations in accordance with ASTM and AAMA standards.

1.4.       SYSTEM DESCRIPTION

  - Design Requirements:

    - Glazing Contractor: Responsible for conforming the system [units], to the architectural plans, including anchorage to structural system and necessary modifications to meet specified requirements and maintain visual design concepts.

    - Drawings: Shop drawings will show the complete assembly installed as described under this section, fully identify all fasteners, glass size and type, shims, gaskets, and hardware required for the complete system installation and be stamped by an engineer licensed in the state where the project is located. Dimensions of all components, alloys, tempers, and finishes will be clearly identified. Provide engineering calculations for all conditions required by the project.

    - Attachment Considerations: Accommodate project design concepts and provide for building movement anticipated from all possible causes. Provide for expansion and contraction in all components to eliminate the possibility of loosening, warping, buckling or bulging of all components.

  - Performance Requirements:

    - Wall-H: The system must be structurally supported.  The fastening system should absorb building movement up to 3/8” (10 mm) + or - 3/16” (5mm) and accept the specified glass thickness.

    - Wall-VH: The system must be structurally supported.  The fastening system should absorb building movement up to 3/8” (10 mm) + or - 3/16” (5mm) and accept the specified glass thickness.

  - Glass Requirements:

    - ANSI Z 97.1 - Glazing Materials Used in Buildings, Safety Performance Specifications and Methods of Test.

    - ASTM C 1036 - Standard Specification for Flat Glass.

    - ASTM C 1048 - Standard Specification for Heat-Treated Flat Glass

    - ASTM C 1172 - Standard Specification for Laminated Architectural Flat Glass.

  - Fitting Support Requirements.

    - The aluminium angle supporting the fittings is pre-treated and powder-coated. Anchors attaching the fittings to the structure must be durable, weather-resistant, and in accordance with corrosion protection class III as per DIN EN 10088 or better. The glass panels must be structurally and durably supported.

- SUBMITTALS

  - [General: Submit in accordance with Section _______.]

  - Product Data: Submit following:

    - Product data sheets for Längle glass fittings and each glass product to be used.

  - Shop Drawings:

    - Submit plan view, elevation details, connection details, and installation details including interface with adjacent construction.

    - Drawings will identify all fittings, gaskets, fasteners, shims, hardware, and accessories used to install the system. They will clearly identify adjacent materials completely and label these materials as “by others”. The drawings will show all dimensions for maximum allowable offset for adjacent components, overall facade alignment tolerance, and maximum allowable deviation of supporting construction from the dimensions shown on the architectural drawings, maximum shim space at anchors etc. [Stamped with seal and signature by registered professional engineer licensed in the jurisdiction where the project is located with a minimum of five (5) years experience in the design of Rain Screen wall systems.]

  - Samples:

    - Glass: Submit three 8” by 8” of standard production material.

    - Fittings: Submit samples for top, bottom and middle attachment.

    - Components: submit samples of all accessories (tapes, shims, gaskets, screws, etc.).

  - Informational Submittals:  Submit following packaged separately from other submittals:

    - Engineering Calculation and Product Information: Submit following:

      - Engineering Calculation showing compliance with specified design requirements and manufacturer’s typical Product Information.

    - Manufacturer’s fabrication and installation instructions.

- QUALITY ASSURANCE

  - Single Source Responsibility: Manufacturer shall be responsible for all fittings components supplied for the basic system and glass if supplied by the fittings manufacturer.

  - [Manufacturer’s authorized representative shall make visits as required to validate warranty.]

  - Welder Qualifications: AWS certified within past 12 months for each type of weld required.

  - Certifications:

    - Certificates verifying AWS qualifications for each welder employed on Project.

- FIELD SAMPLES

  - [General: Comply with Section ______.]

  - [Sample Installation:]

    - [Install one full size [      ] wide by [      ] long in location as directed by Architect.]

    - [Show hardware, accessories and construction techniques.]

    - [Accepted Field Sample: May remain part of completed work and will serve as criteria for visual acceptance for the project.]

- MOCK – UPS

  - [General: Comply with Section ______.]

  - [Testing Laboratory Mock-Up: (Not required)]

    - Construct mock-up ____ feet high by ____ feet wide as indicated.

    - Locate at certified independent testing laboratory as selected by Architect.

    - Perform tests in accordance with [__________].

  - Visual mock-Up/Field Sample: (Not required).

    - Construct typical, full size mock-up panel.

    - Locate as directed by Architect.

    - [Perform following field tests in order listed:]

      - [_________________________________].

      - [_________________________________].

    - Accepted Mock-Up/Field Sample: May [not] remain part of completed work.

- PRE-INSTALLATION CONFERENCE

  - [Conduct pre-installation conference in accordance with project requirements.]

  - Identify access to site, storage, sequencing, and scheduling.

  - Establish requirements for visits by manufacturer’s representative.

- DELIVERY, STORAGE, AND HANDLING

  - General: Store in manufacturer’s unopened packaging on a level surface, above ground, in a watertight enclosed space fully ventilated and protected from damage and in accordance with manufacturer’s recommendations.

  - All glass products to be fully protected from impact and staining or spotting

- WARRANTY

  - Special Warranty:

    - Warrant installed units to be free from defects in material and workmanship for a period of maximum of 5 years. Include coverage against crack, warp, pit, corrode, peel, or blister under normal use and service.

    - Installation warranty of [_____] year(s) shall be supplied by selected glazing contractor.

PART 2 	         PRODUCTS

- MANUFACTURERS AND PRODUCTS

  - Basis-of-Design Product:

The design is based on Bendheim Wall Systems, Inc. (BWS) with aluminum fittings by LängleGlas. BWS is Located at 61 Willett Street, Building J, Passaic, NJ  07055. Tel: 800-221-7379 Fax: 973-458-0233 Email: rainscreens@bendheim.com Subject to compliance with requirements, provide the named product or a comparable product by one of the following.

    - LängleGlas

    - No [known] Substitutions.

    - [Accepted Substitute in accordance with Section ______.]

  - Glass Products:

  - Glass type, per BWS glass samples provided to the architect.

  - Fittings and glass products of other manufacture’s matching the aesthetics, performance, and certifications of the above listed specified products will be considered for approval if submitted as part of the bid proposal and accompanied by samples, performance data, certifications and written statement that the manufacturer will conform to all requirements of these Specifications.

- MATERIALS

  - Aluminum Fittings and Glass:

    - Wall-H: 3/4” Horizontal overlap aluminum fasteners are Alloy 6063-T6 in accordance with DIN 18516 Part 4. The bolt connecting the fasteners to the aluminum angle is stainless steel 5/16” (M8) diameter with washer in accordance with DIN 933 or per the project engineer.

    - Wall-VH: 3/4” horizontal overlap and 1 3/16” vertical overlap aluminum fasteners are Alloy 6063-T6 in accordance with DIN 18516 Part 4. The bolt connecting the fasteners to the aluminum angle is stainless steel 5/16” (M8) diameter with washer in accordance with DIN 933 or per the project engineer.

    - Glass: Per BWS glass sample provided to the architect

  - FABRICATION

  - Coordination of Fabrication: Check all field conditions for acceptable conformance to the architectural drawings.

  - General:

    - Install fittings as shown on the shop drawings and in accordance with the manufacturer’s assembly instruction.

    - Isolate dissimilar metals and aluminum in contact with concrete utilizing protective coating or pre-formed separators which will prevent contact and corrosion.

  - Welding: Comply with recommendations of American Welding Society (AWS).

    - Use recommended electrodes and methods to avoid distortion and discoloration.

    - Grind exposed welds smooth and flush with adjacent surfaces; restore material finish.

2.4        FINISHES

  - Powder coated RAL [       ].

  - [Clear Anodized: AA-M12C22A41, Architectural Class 1, etched, medium matte, clear anodic coating, 0.7 mil [(0.018mm)] minimum thickness.

PART 3 EXECUTIONS

3.1       INSTALLERS

  - Architect [Engineer] approved [with a minimum of (5) years experience in the installation of glazing systems].

3.2       EXAMINATION

  - Do not begin installation until substrates have been suitably prepared to accommodate the system.

  - Examine and verify substrate surfaces to receive the Rain Screen system, associated work, and conditions where work will be installed are in conformance with approved plans.

  - Maximum deviation from vertical and horizontal alignment of substrate shall be no more than 1/4” in 20 feet (1 mm in 1 m).

  - Do no proceed with work until unsatisfactory conditions have been corrected in a manner acceptable to installer. Starting work within a particular area will be construed as installer’s acceptance of surface conditions.

  - If substrate preparation is the responsibility of another installer, notify architect/engineer of unsatisfactory preparation before proceeding.

3.3      PREPARATION

  - Protection: [_________________________________].

  - Surface Preparation: [_______________________________].

3.4       INSTALLATION

  - Install units in accordance with approved Shop Drawings, plumb, level, square, free from warp or twist while maintaining dimensional tolerances, alignment with surrounding construction [adjacent surfaces] and [Section _____], [State/Jurisdiction of ______ standards], manufacturer’s assembly manual.

  - Erect fasteners and glass in accordance with manufacturer’s printed installation instructions. Clean glass immediately before installing.

3.5        FIELD QUALITY CONTROL

  - [Manufacturer’s Field Services: Comply with Section _____.]

    - Employ manufacturer’s representative as necessary to insure proper installation and to verify work is done in accordance with manufacturer’s requirements.

3.6       CLEANING

  - Cleaning: [Comply with Section _______.]

    - Clean as recommended by manufacturer. Do not use materials or methods which may damage system components or surrounding construction.

  - PROTECTION

  - Protection: [Protect finished work in accordance with Section_____.]

    - Protect finished surfaces from damage.

END OF SECTION